RFP Form for egeplast 9010® RCplus Drinking Water Pipe

Preliminary note:

Drinking water pipe in accordance with DIN 8074/8075, DIN EN 12201 for installation without a sand bed, made of PE 100-RC with the highest resistance to slow crack growth (FNCT minimum requirement: ≥ 8760 h in accordance with DVS 2203-4; T=80°C, σ=4 N/mm2, 2% Arkopal), 90% of the nominal wall thickness black, 10% of the nominal wall thickness on the outside blue to identify the medium as drinking water. Verified in accordance with both DIN 8075 and DVGW GW 335 Part A2, with an integrated 10% coloured indicator layer, included in the nominal dimensions, on the outside, to facilitate an accurate assessment of the pipe surface as required by the relevant regulating bodies.

An approval for the medium drinking water is existent. Piping construction according to PAS 1075 Type 2, pipe with dimensions according to DIN 8074, double layered piping with integrated protective layer made of PE 100 or PE 100-RC and having an internal co-extruded protective layer of PE 100-RC.

The monitoring of constant material quality acc. to PAS 1075 is carried out by an independent testing and inspection institute which is accredited by the “Deutsches Institut für Bautechnik” DIBT (German approval body for construction products an types of construction), Berlin .

The suitability of the product for installation without a sand bed is verified by an independent assessor. All necessary pipeline joints created by means of either electrofusion welding or butt fusion welding are to be made according to the requirements of the applicable DVS technical guidelines. The piping is to be stored and transported on the building site in compliance with the KRV guidelines.

Product:	egeplast 9010® RCplus drinking water pipe

made of PE 100-RC or equivalent

Manufacturer:	egeplast international GmbH

Robert-Bosch-Str. 7

D-48268 Greven, Germany

Tel.: +49.2575.9710-0		Fax: +49.2575.9710-110

e-mail: info@egeplast.de

http://www.egeplast.de 		http://www.egeplast.eu

Specification of services:	egeplast 9010® RCplus drinking water pipe made of PE 100-RC with dimensions: ________mm, SDR _____

delivered as straight lengths of 6 / 12 m

delivered as bundled coils in lengths_____ of m

Deliver_______ running metres and install professionally according to DIN and appropriate installation guidelines as drinking water pipe:______________ € / running metre

### RFP Form for egeplast 9010® RCplus Gas Pipe

Preliminary note:

Gas pipe in accordance with DIN 8074/8075, DIN EN 1555 for installation without a sand bed, made of PE 100-RC with the highest resistance to slow crack growth (FNCT minimum requirement: ≥ 8760 h in accordance with DVS 2203-4; T=80°C, σ=4 N/mm2, 2% Arkopal), 90% of the nominal wall thickness black, 10% of the nominal wall thickness on the outside orange to identify the medium as natural gas. Verified in accordance with both DIN 8075 and DVGW GW 335 Part A2, with an integrated 10% coloured indicator layer, included in the nominal dimensions, on the outside, to facilitate an accurate assessment of the pipe surface as required by the relevant regulating bodies.

An approval for the medium gas is existent. Piping construction according to PAS 1075 Type 2, pipe with dimensions according to DIN 8074, double layered piping with integrated protective layer made of PE 100 or PE 100-RC and having an internal co-extruded protective layer of PE 100-RC.

The monitoring of constant material quality acc. to PAS 1075 is carried out by an independent testing and inspection institute which is accredited by the “Deutsches Institut für Bautechnik” DIBT (German approval body for construction products an types of construction), Berlin .

The suitability of the product for installation without a sand bed is verified by an independent assessor. All necessary pipeline joints created by means of either electrofusion welding or butt fusion welding are to be made according to the requirements of the applicable DVS technical guidelines. The piping is to be stored and transported on the building site in compliance with the KRV guidelines.

Product:	egeplast 9010® RCplus gas pipe

made of PE 100-RC or equivalent

Manufacturer:	egeplast international GmbH

Robert-Bosch-Str. 7

D-48268 Greven, Germany

Tel.: +49.2575.9710-0			Fax: +49.2575.9710-110

e-mail: info@egeplast.de

http://www.egeplast.de 			http://www.egeplast.eu

Specification of services:	egeplast 9010® RCplus gas pipe made of PE 100-RC with dimensions:________mm, SDR _____

delivered as straight lengths of 6 / 12 m

delivered as bundled coils in lengths of______ m

Deliver running _____metres and install professionally according to DIN and appropriate installation guidelines as gas pipe:____________ € / running metre

RFP Form for egeplast 9010® RCplus Sewage Pressure Pipe

Preliminary note:

Sewage pressure pipe in accordance with DIN 8074/8075, DIN EN 12201 for installation without a sand bed, made of PE 100-RC with the highest resistance to slow crack growth (FNCT minimum requirement: ≥ 8760 h in accordance with DVS 2203-4; T=80°C, σ=4 N/mm2, 2% Arkopal), 90% of the nominal wall thickness black, 10% of the nominal wall thickness on the outside brown to identify the medium as sewage. Verified in accordance with DIN 8075, SKZ monitored, with an integrated 10% coloured indicator layer, included in the nominal dimensions, on the outside, to facilitate an accurate assessment of the pipe surface as required by the relevant regulating bodies.

Piping construction according to PAS 1075 Type 2, pipe with dimensions according to DIN 8074, double layered piping with integrated protective layer made of PE 100 or PE 100-RC and having an internal co-extruded protective layer of PE 100-RC.

The monitoring of constant material quality acc. to PAS 1075 is carried out by an independent testing and inspection institute which is accredited by the “Deutsches Institut für Bautechnik” DIBT (German approval body for construction products an types of construction), Berlin .

The suitability of the product for installation without a sand bed is verified by an independent assessor. All necessary pipeline joints created by means of either electrofusion welding or butt fusion welding are to be made according to the requirements of the applicable DVS technical guidelines. The piping is to be stored and transported on the building site in compliance with the KRV guidelines.

Product:	egeplast 9010® RCplus sewage pressure pipe

made of PE 100-RC or equivalent

Manufacturer:	egeplast international GmbH

Robert-Bosch-Str. 7

D-48268 Greven, Germany

Tel.: +49.2575.9710-0		Fax: +49.2575.9710-110

e-mail: info@egeplast.de

http://www.egeplast.de 		http://www.egeplast.eu

Specification of services:	egeplast 9010® RCplus sewage pressure pipe made of PE 100-RCwith dimensions: ________mm, SDR _____

delivered as straight lengths of 6 / 12 m

delivered as bundled coils in lengths_____ of m

Deliver_______ running metres and install professionally according to DIN and appropriate installation guidelines as sewage pressure pipe:______________ € / running metre